## Slide 1: TFF Capture of Exosomes with Ultrathin Membranes
(A) Capture stage
(B) Clean-up stage
(C) Collection stage
(D) Schematic of a chip based device with microfluidic access at the inlet and outlet of top and bottom chambers
Isolation of exosomes on nanomembranes by diffusion-driven physical sieving in a modified tangential flow device:

## Slide 2: Optimization of TFF Device
30 microliter, 30 minutes
60 microliter, 60 minutes
90 microliter, 90 minutes
120 microliter, 120 minutes

## Slide 3: Optimization of TFF Device
Before Washing
After Washing
Average Intensity: 7.780
Average Intensity: 6.265

## Slide 4: Optimization of TFF Device
Before Releasing
After Releasing
Average Intensity: 5.647
Average Intensity: 6.265

## Slide 5: Optimization of TFF Device
Having an air bubble

## Slide 6: Track Etched Membranes
Verification of our approach: single step tangential flow concept.
Different pore sizes: 10, 50, 80, 100, and larger
Upside down, changing the design
Compare and show advantageous of our membranes over TE membranes
Clamped devices

## Slide 7: TE membrane

## Slide 8: Trapping Step
40 Microliter
60 Microliter
80 Microliter
Average Intensity: 275.359
Average Intensity: 291.365
Average Intensity: 360.944

## Slide 9: Washing Step
Before Washing
After Washing
Average Intensity: 360.944
Average Intensity: 340.723

## Slide 10: Releasing Step
Before Releasing
After Releasing
Average Intensity: 340.723
Average Intensity: 291.469

## Slide 11: Washing after Releasing
Before Washing
After Washing
Average Intensity: 291.469
Average Intensity: 285.918