## Slide 1: Silicon Nanomembranes as an Enabling Platform for Multifunctional Microsystems
Greg Madejski, University of Rochester, Biomedical Engineering

## Slide 2: Si Nanomembrane Technology
Silicon filter material
          thin (50 nm)
          highly porous
          chemically stable
          mechanically robust
          scalable manufacturing
a) van den Berg and M. Wessling, Nature 2007, b) Streimer, Nature 2007
Notes: I work with silicon nanomembranes, based off a discovery by chris striemer back in 2007. He took a very thin sheet of silicon (50nm) and heated it up quickly to form little nanocrystals. Exposing the thin sheet of silicon revealed voids in the material, creating nanopores. There are many advantages to this kind of filter compared to a traditional polymer membrane.

## Slide 3: Si Nanomembrane Applications
Gaborski, T. R., et al. (2010). "High-Performance Separation of Nanoparticles with Ultrathin Porous Nanocrystalline Silicon Membranes." ACS Nano 4(11): 6973-6981
Notes: We can use nanomembranes for a variety of operations. Pumping via electroosmosis, pure physical separation, electrostatic gating, and as a scaffold to promote cell growth in a permeable way.

## Slide 4: Si Nanomembrane Applications
Kavalenka, M. N., et al. (2012). "Chemical capacitive sensing using ultrathin flexible nanoporous electrodes." Sensors and Actuators B: Chemical 162(1): 22-26
Notes: We can use nanomembranes for a variety of operations. Pumping via electroosmosis, pure physical separation, electrostatic gating, and as a scaffold to promote cell growth in a permeable way.

## Slide 5: Si Nanomembrane Applications
Snyder, J. L., et al. (2013). "High-performance, low-voltage electroosmotic pumps with molecularly thin silicon nanomembranes." Proceedings of the National Academy of Sciences 110(46): 18425-18430.
Notes: We can use nanomembranes for a variety of operations. Pumping via electroosmosis, pure physical separation, electrostatic gating, and as a scaffold to promote cell growth in a permeable way.

## Slide 6: Si Nanomembrane Applications
Agrawal, A. A., et al. (2010). "Porous nanocrystalline silicon membranes as highly permeable and molecularly thin substrates for cell culture." Biomaterials 31(20): 5408-5417
Notes: We can use nanomembranes for a variety of operations. Pumping via electroosmosis, pure physical separation, electrostatic gating, and as a scaffold to promote cell growth in a permeable way.

## Slide 7: Si Nanomembrane Applications
Chung et al. “Highly Permeable Silicon Membranes for Shear-free Chemotaxis and Cell Labeling” Lab Chip 2014
Cells
Tangential Flow
106 fold shear stress reduction
Notes: Dr. Henry Chung published in Lab on a Chip where he used the properties of nanomembranes to effectively shield cells from fluid shear stress. This kind of protective effect would be really useful for other kinds of devices that are sensitive to flow or get gummed up by nonspecific binding. In other words the membrane could act as an upstream filter and still shield any device place underneath it.

## Slide 8: Microsystem
Microsystem
Pump
Sensor
Filter
Support
Miniaturized
Efficient
Parallelizable
Repeatable
Notes: A Microsystem combines many different elements to perform different processes that gain us better information or build us on a small scale. Because the activities are miniaturized, they are generally efficient compared to their counterparts, and they can be designed for repeatability and parallelization to take advantage of the minimal resources they consume individually.

## Slide 9: Integrated Nanomembrane Microsystem
EO Pump
Cell Substrate
Filter A
Filter B
Filter C
Flow Sensor
10 mm
Hundreds of microsystems fabricated at once
Notes: All of these functions lead to my vision of a system where you can control these different functions and integrate them onto a single chip. Micrototal analysis systems, or ‘Lab on a chip’ type systems minaturize and combine all of these applications. Explain image

## Slide 10: Lab-on-a-Chip (LOC)
“Membrane may shrink Lab-on-a-chip power source”, University of Rochester Currents, 11/23/13, Vol. 41, No. 3
Notes: Integrating all of these functions together to tackle a biomedical problem puts us squarely in the realm of Lab on a chip systems. Here’s an picture of a simple silicon nanomembrane that’s been combined with silicone microfluidic channels that can fit onto a microscope slide. Putting many different operations into a small space can be complicated

## Slide 11: Lab-off-a-Chip
Pump
Filter
Cell Culture
Microfluidic
Tubing
Notes: It’s difficult to fit all of the necessary microsystem operations in the same place. These are not neglectable decisions, especially when dealing in the confined space of a microscope.

## Slide 12: Existing Pumping Technology
Pneumatic PDMS
75 μL/min
Bulky additional control hardware
Backend integration complexity
Ni, J., et al. (2012).
Microelectronic Engineering 99: 28-32

## Slide 13: Existing Pumping Technology
Photoresist EO
~1 μL/min, 10 V
Inefficient Pumping
10 Pa stall pressure
Jahanshahi, A., et al. (2012).
Microfluidics and Nanofluidics 12(5): 771-777.

## Slide 14: Existing Miniaturization
Al-Rjoub, M. F., et al. (2015). "Improved Flow Rate in Electro-Osmotic Micropumps for Combinations of Substrates and Different Liquids With and Without Nanoparticles." Journal of Electronic Packaging 137(2): 021001-021001.
500 V
~75 μL/min
Flow meter is bigger than the device!

## Slide 15: What can be done better?
Create a generalizable Microsystems Platform
Simple miniaturization – small components, not a lot of supporting equipment, low dead volume
Design cues – connect pump regions, filter regions, sensor regions together
Compatible with existing
technology, materials, procedures
EO Pump
Cell Substrate
Filter A
Filter B
Filter C
Flow Sensor

## Slide 16: What applications could be improved?
Add protection layers to sensors
  DNA Sequencing
  Photonics
Multimodal sensing in a confined space
  Tissue on a chip
  Concurrent optical, electrical, physical sensing under a microscope
Individualized miniature pumps/sensors
Notes: Upon the successful completion of these aims we will have achieved….

## Slide 17: Aims
Aim 1 – Fabrication of Nanomembrane Tented Structures to Extend the Lifetime of Delicate Sensing Devices
Aim 2 – Fabrication of Raman-Silent Nanomembranes to Enable the Chemical Fingerprinting of Cellular Components by Raman Spectroscopy
Aim 3 – Integration of Nanomembrane Operations to Create a Multimodal Measurement System for the Study of Water Transport through Retinal Epithelial Monolayers
Notes: I hope to demonstrate these characteristics through three aims that tackle problems in biomedical LOC settings.

## Slide 18: Aims
Aim 1 – Addition of a nanofilter into existing process
Aim 2 – Bottom up fabrication of new nanomembrane materials
Aim 3 – Combine nanomembrane functions to build a miniaturized fluid transport model
Notes: Translating those titles a little, the chief microsystem activities we want to achieve here are

## Slide 19: Tents, New Materials, Epithelial LOC
Si
Si
50 nm NPN
50 nm MgF2
Evaporation
RIE
Aim 1
Aim 2
Aim 3
Notes: Nanofilter protecting delicate sensor underneath.

## Slide 20: DNA Nanopore Sequencers
Alpha Hemolysin
Branton, D., et al. (2008). "The potential and challenges of nanopore sequencing." Nat Biotech 26(10): 1146-1153.
Biological Nanopore, ~$1000/genome, Oxford Nanopore
Notes: A large area of biomedical microsystem literature is devoted to DNA sequencing. DNA nanopore sequencers promise to usher in an age of personalized medicine, where individual genomes are sequenced cheaply and effectively to make better healthcare decisions. The dominant commercial technology, through a biological protein-based nanopore is approaching about $1000/genome.

## Slide 21: DNA Nanopore Sequencers
Dekker, C. (2007). "Solid-state nanopores." Nat Nano 2(4): 209-215.
Single Silicon Nanopore
Cheap Fabrication
Stable Shelf Life
Poor base pair resolution
Single point of failure
Notes: Newer silicon nanopore technology is being developed as a lower-cost, more stable alternative, as you don’t have to worry about the condition of the biological pore.

## Slide 22: DNA Blockage
A filter could screen out ‘clogging’ DNA configurations
Schneider, G. F., et al. (2013). "Tailoring the hydrophobicity of graphene for its use as nanopores for DNA translocation." Nat Commun 4.
Notes: Unfortunately, these devices have a major limitation; a single point of entry. This means that if DNA gets balled up, or garbage gets near the device, the DNA sensor would stop working.

## Slide 23: Nanomembrane-Vapor Transfer

## Slide 24: Tenting
Notes: Tenting video, dropping a thin sheet of nanoporous membrane on top of a structure to protect devices underneath it.

## Slide 25: Tenting - SEM

## Slide 26: Tenting - Wetting
Notes: Repeated applications of water vapor swell the nanomembrane, but ultimately is fixed in place. Water can diffuse into cavity spaces

## Slide 27: Tenting - Wetting
Notes: The wetting behavior is unusual. The NPN and silicon nitride are the same material composition, but display different wetting behavior

## Slide 28: Tenting - Wetting
Notes: Nonporous membranes actually can trap water underneath. Gif shows fluorophore diffusing around underneath a nonporous membrane

## Slide 29: Tent Stability
Stability under shear stress
3 dynes/cm2
Notes: The perturbation into the fluid flow is small, stable under shear stress.

## Slide 30: Tenting – Adhesion Model
Stable for a week, submerged in water
Water provides adhesion
Notes: We need to know more about this process in order to integrate it into other flows potentially.

## Slide 31: Tenting – Adhesion Model
Si3N4
NPN
Intermolecular Forces
VanDerWaals Forces
Hydrogen Bonding
Dipole-Dipole Interaction
Si3N4
NPN
Si3N4
NPN
vs
vs

## Slide 32: Tented Filtration
60 nm Au
aggregate
Notes: Filtering out aggregates is important analagous to DNA coiling on itself

## Slide 33: Tented Filtration
Notes: Small pieces can still get through!

## Slide 34: Tented Nanopore Sequencing
Tent in Place
Extend the lifetime of silicon nanopore sequencers

## Slide 35: Aim 1 Summary
Integrating nanomembranes into microsystems will allow us to create/improve multifunctional microsystems (tenting protects devices)
However, silicon is not always the optimal material choice for the application at hand!

## Slide 36: Tents, New Materials, Epithelial LOC
Si
Si
50 nm NPN
50 nm MgF2
Evaporation
RIE
Aim 1
Aim 2
Aim 3
Notes: All of these functions lead to my vision a system where you can control these different functions and integrate them onto a single chip. Micrototal analysis systems, or ‘Lab on a chip’ type systems minaturize and combine all of these applications. The creation of tissue models within these microsystems are often referred to as organ on a chip models. I am particularly interested in models of water transport in an in vitro model of the retina. With nanomembranes having so much functionality, it should be easier to remove macroscopic pumps and sensors and produce high fidelity information. More information on this later.

## Slide 37: Retinal Pigment Epithelium (RPE)
de Jong, P. T. V. M. (2006). "Age-Related Macular Degeneration." New England Journal of Medicine 355(14): 1474-1485.
Keeps the photoreceptors alive
Governs the transport of nutrients into and water out of the outer retina space
Digests old photoreceptor segments
Notes: Macular degeneration causes people to go blind. Compared to the retina of a 3-year old, a dysfunctional RPE causes photoreceptors to die off. The accumulation of Drusen is the classic symptom of this disease, yellowish deposits underneath the RPE. AS the RPE maintains the health of the outer retinal, it governs the flow of water and solutes into the outer retinal space.

## Slide 38: RPE Ocular Disease
de Jong, P. T. V. M. (2006). "Age-Related Macular Degeneration." New England Journal of Medicine 355(14): 1474-1485.
Transport is compromised
Photoreceptor health is not maintained
Photoreceptor death leads to blindness
Notes: Macular degeneration causes people to go blind. Compared to the retina of a 3-year old, a dysfunctional RPE causes photoreceptors to die off. The accumulation of Drusen is the classic symptom of this disease, yellowish deposits underneath the RPE. AS the RPE maintains the health of the outer retinal, it governs the flow of water and solutes into the outer retinal space.

## Slide 39: Water Transport Physiology
Pffefer and Philp, “Cell Culture of the Retinal Pigment Epithelium”, Experimental Eye Research, 2014
Outer Retina
Retinal Pigment Epithelium
in Vitro
Needs a permeable support for proper morphology
H2O
Notes: I am particularly interested in models of water transport in an in vitro model of the retina. With nanomembranes having so much functionality, it should be easier to remove macroscopic pumps and sensors and produce high fidelity information. RPE nourishes the photosensitve cells in the back of the retina, and supports it.

## Slide 40: Raman Theory
“Chemically sensitive bioimaging with coherent Raman scattering”, Camp and Cicerone, Nature Photonics, 2015
Notes: I am interested in eye physiology and water transport. One technique that we can use to directly observe water transport is known as Raman spectroscopy. The process works off of a phenomenon known as the Raman shift. Most light is scattered elastically, that is green light scatters off a surface and remains green. But every one in few million photons comes out either blue or red. This inelastically scattered light can tell us what was illuminated. By collecting all the colors of light, we can create a spectrogram of the material.

## Slide 41: Raman Theory
‘Characterizing Carbon Materials with Raman Spectroscopy’ Joe Hodkiewicz, Thermo Fisher Scientific, Madison, WI, USA, App #51901
Notes: Not all materials behave the same. Raman responds to molecular bond orientation. Here we have group 4 elements all producing a strong characteristic spike., shifted along different wavelengths.

## Slide 42: Raman Theory
‘Characterizing Carbon Materials with Raman Spectroscopy’ Joe Hodkiewicz, Thermo Fisher Scientific, Madison, WI, USA, App #51901
Notes: All of the signals can add, and you can discriminate what is in the observation volume by pulling apart the superimposed signatures.

## Slide 43: Raman Theory
Notes: Not all materials behave the same. Even allotrophic forms of carbon produce wildly different signatures.

## Slide 44: Imaging Water Transport by Raman
Potma, E. O., et al. (2001). "Real-time visualization of intracellular hydrodynamics in single living cells." Proceedings of the National Academy of Sciences 98(4): 1577-1582.
D2O
Notes: If you take a line scan above a bunch of isolated cells, you can observe the ratio of Deuterium to Water change

## Slide 45: Imaging Water Transport by Raman
Potma, E. O., et al. (2001). "Real-time visualization of intracellular hydrodynamics in single living cells." Proceedings of the National Academy of Sciences 98(4): 1577-1582.
Experimental
Simulation
Notes: If you lump together a bunch of these cells, you can calculate a time constant for water moving through the cells. A) experimental data, B) a simulation with a permeability of 2.2 um/s

## Slide 46
Raw
DNA
RNA
Brightfield
2d Raman
Si Nanomembrane
Si Nanomembrane + Cell
High background signal from Si
Measurement takes 2.5 hours!
Remove Si, make faster measurements

## Slide 47: Fabrication - Strategy
Si
Si
50 nm NPN
50 nm MgF2
Evaporation
RIE

## Slide 48: Fabrication - Structure
Nanopore Filling
Si
Si
50 nm NPN
50 nm MgF2
Evaporation
RIE
Anneal, 700 C, 2 hrs

## Slide 49: Electron Micrographs

## Slide 50: Material - EDS
Over 85% MgF2

## Slide 51: Material - XPS

## Slide 52: Mechanical Strength

## Slide 53: Cytocompatibility
P5 HUVECs on nanoporous
MgF2

## Slide 54: Membrane Durability Under Laser Exposure
450 mW
15x Power vs pnc-Si = 15x Quicker Measurements
30 mW
pnc-Si
MgF2

## Slide 55: Reduction of Silicon Peak

## Slide 56: Fabrication – Au, Pt
Nanopore Filling
Si
Si
50 nm NPN
50 nm Au
Evaporation
RIE

## Slide 57: Aim 2 Summary
Silicon nanomembrane physical characteristics can be transferred into other material systems, enabling Raman microscopy to be used on this microsystem platform

## Slide 58: Tents, New Materials, Epithelial LOC
Si
Si
50 nm NPN
50 nm MgF2
Evaporation
RIE
Aim 1
Aim 2
Aim 3

## Slide 59: Electroosmotic Pumping
Snyder, J. L., et al. (2013). "High-performance, low-voltage electroosmotic pumps with molecularly thin silicon nanomembranes." Proceedings of the National Academy of Sciences 110(46): 18425-18430.
Notes: Rice-Whitehead theory

## Slide 60: EO Flow
Pore Wall

## Slide 61: Electroosmotic Pumping
Snyder, J. L., et al. (2013). "High-performance, low-voltage electroosmotic pumps with molecularly thin silicon nanomembranes." Proceedings of the National Academy of Sciences 110(46): 18425-18430.

## Slide 62: Streaming Potential Sensor
Run the electroosmotic pump in reverse
Park, H. and S.-H. Choa (2014). "Measurement of liquid flow rate by self-generated electrokinetic potential on the microchannel surface of a solid." Sensors and Actuators A: Physical 208: 88-94.

## Slide 63: 3d Printed Microsystem

## Slide 64: Cell Growth
PolyLactic Acid 3d printed, fits in a 24 well plate
Transfer cells after cell confluence

## Slide 65: Resealable Microsystem
Bottom
Open
Top

## Slide 66: Water Transport Measurement
NPN Pumps
MgF2 Cytoscaffold
NPN Flow Sensor
Raman D2O/H2O

## Slide 67: Combined Measurements
Raman D2O/H2O
Manipulate the epithelial pumping rate
  Osmotic Challenge
  pH Challenge
  Stall Pressure (EO pump)
Measure water flow through streaming potential sensors
Mechanical Challenge

## Slide 68: Tents, New Materials, Tissue LOC
Si
Si
50 nm NPN
50 nm MgF2
Evaporation
RIE
Notes: Upon the successful completion of these aims we will have achieved….

## Slide 69: Summary
Integrate different nanomembranes to improve microsystem characteristics
  Pumping Regions
  Protection Regions
  Sensing Regions
  Supporting Regions
Create a generalizable Microsystems Platform
Simple miniaturization – small components, not a lot of supporting equipment, low dead volume
Compatible with existing
technology, materials, procedures

## Slide 70: Acknowledgements
University of Rochester
Prof. James McGrath
Dean Johnson, PhD
Joshua Winans, PhD
Henry Chung, PhD
Tejas Khire
Karl Smith
Sarah Wayson
Meghan Kazanski
Tucker Burgin
J.P. DesOrmeaux
Josh Miller
Jamie Roussie, PhD
RIT
Prof. Tom Gaborski
Bob Carter, PhD
University of Nottingham
Prof. Kevin Webb
Flavius Pascut, PhD
Emilia Moradi, PhD
University of Ottawa
Prof. Vincent Tabard-Cossa
Kyle Briggs
URnano – Brian McIntyre

## Slide 71: Questions?