## Slide 2
1D and 2D nanosieves
circular pores
45 nm thickness, 120 nm diameter
3.2 % porosity
flux and selectivity at different pressures are mesured
Transition flux is a linear addition of viscous and molecular fluxes, proved w/o fitting parameters

## Slide 3: Fabrication
nanosieve (120 nm pore diameter)
  Silicon nitride 45nm LPCVD deposited (future membrane)
  Laser interference lithography (LIL) to create pore pattern
  Plasma etch to make pores
microsieve (6 micron pore diameter)
  Pores etched by deep reactive-ion etching DRIE
nanosieve and microsieve fusion bonded
nanosieve wafer carrier is etched away
  thermal oxide acts as stop layer which is removed after

## Slide 4
nanosieve
microsieve support

## Slide 5: Device Fabrication
3.2% final porosity
glass tube of 3mm diameter fusion bonded to microsieve to measure gas flow

## Slide 6: Theory and Characterization
viscous (Kn < 0.01), transition (0.01 < Kn < 1) and molecular (Kn > 1) flow regime, Knudsen number: Kn = λ/d
Knudsen described transition flow as superimposition of viscous and molecular flows, included wall interaction correction terms

## Slide 7: Theory and Characterization
ΔP- pressure drop (Pa), Ф – mass flow (mol/s), F – flow conductance (mol/s/Pa)

## Slide 8: Theory and Characterization
ΔP- pressure drop (Pa), P- mean pressure (Pa)

## Slide 9
MOLECULAR FLOW
VISCOUS FLOW

## Slide 10
Pure gas flow experiments
Lager selectivity for higher Kn numbers
He/Ar selectivity is 3.1 at 20 mbar (close to theoretic) – molecular regime
2.39 at 1 bar due to viscosity differences b/w gases, it will disappear whith mixtures
Total strength is 5 bar and more

## Slide 11: Gas permeability paper plan

## Slide 12
Membrane, characterization, air permeability values (compared)
Gas transport in restricted geometries, Knudsen diffusion theory, pore processing + modeling molecular flow, theoretical and experimental data correlation, no pressure dependence, porosity determination and possible quality testing (pressure dependence if pinholes-viscous flow)
Single gas selectivities due to Knudsen diffusion (He, Co2, N2)
Probability of collision-free passage of gas molecule, enhancement in permeabilities of membranes with the same porosity but different average pore diameters

## Slide 13: Gas Selectivity and M Dependence Experiments
CO2
N2
He
Experimental M dependence for
membranes with different porosities
He
N2
CO2
Single gas selectivities , experimental
and Knudsen prediction
N2/Co2 average=1.1950, theory =1.2536, error=5%
N2/He average=0.3993, theory= 0.3780, error=5%
Co2/He average=0.3355, theory=0.3015, error=10%

## Slide 14: Collision-free transport
Average percent of molecule trajectories
which pass the pore certain diameter and
height without hitting a wall

## Slide 15: Permeability enhancement
Permeabilities of membranes with close
starting porosities, averaged to 1 % plotted
against average pore diameter. Calculated
value consists of sum of weighted
collision-free (Clausing factor=1) and
Knudsen permeabiliies calculated for
particular membrane.
different starting porosities

## Slide 16: Paper Plan
1
2
3
4