## Slide 1: SERS Sensing
Greg Madejski, University of Rochester, Biomedical Engineering

## Slide 2: Sensing
Development of a non-silicon nanomembrane for Raman-compatible cell-culture
Development of a novel Raman sensing structure for sensitive identification of molecules
Si
Si
MgF2
MgF2
Au

## Slide 3: Si Nanomembrane Applications
Gaborski, T. R., et al. (2010). "High-Performance Separation of Nanoparticles with Ultrathin Porous Nanocrystalline Silicon Membranes." ACS Nano 4(11): 6973-6981
Notes: We can use nanomembranes for a variety of operations. Pumping via electroosmosis, pure physical separation, electrostatic gating, and as a scaffold to promote cell growth in a permeable way.

## Slide 4: Si Nanomembrane Applications
Kavalenka, M. N., et al. (2012). "Chemical capacitive sensing using ultrathin flexible nanoporous electrodes." Sensors and Actuators B: Chemical 162(1): 22-26
Notes: We can use nanomembranes for a variety of operations. Pumping via electroosmosis, pure physical separation, electrostatic gating, and as a scaffold to promote cell growth in a permeable way.

## Slide 5: Raman Sensing: SERS
Surface Enhance Raman Spectroscopy
  Roughened metals have sharp features that can condense an electric field around them
  Raman Scattering Effect is proportional to the strength of the electric field
  Enhancement factors can be enormous, up to 1,000,000x better

## Slide 6: SERS Plasmonics
J. M. McMahon, S. Li, L. K. Ausman and G. C. Schatz, J. Phys. Chem. C, 2012, 116, 1627–1637
WaveNET Tank Testing :: FloWaveTT 2014, Edinbugh University
Notes: Electron oscillation produces a stronger electric field from a traveling wave

## Slide 7: How is SERS Useful?
Detect many different molecules simultaneously
  Excellent specificity and resolution (fM-pM)
  Glucose, Residue, Food-Safety

## Slide 8: Raman Sensing: SERS
Hsin-Hung Cheng et al. "Effects of the tip shape on the localized field enhancement and far field radiation pattern of the plasmonic inverted pyramidal nanostructures with the tips for surface-enhanced Raman scattering," Opt. Express 19, 22125-22141 (2011)
Sharper features will produce a stronger enhancement
Modification of commercial Klarite SERS substrate
Notes: Scale is logarithmic: eg 1=10x stronger 2=100x stronger

## Slide 9: Metallic SERS Structures
“Recent Progress in SERS Biosensing”, Phys Chem Chem Phys. 2011 June 28; 13(24): 11551–11567. doi:10.1039/c0cp01841d
Nanosphere
Nanoshell
Nanowire
Nanohole
Nanotip

## Slide 10: NanoVolcanoes
MgF2 Infill from production produces conical structures
30 nm height
Can I make a nanomembrane like this out of Au?

## Slide 11: Fabrication – Au, Pt
Nanopore Filling
Si
Si
50 nm NPN
50 nm Au
Evaporation
RIE
5.4 x 5.4 mm chips

## Slide 12: Freestanding Au Nanomembranes
Freestanding 50 nm Au

## Slide 13: Freestanding Au Nanomembranes
Rough Structures Evident in Crossection
Extremely flimsy – 50 nm of holey gold

## Slide 14: Adding Au to MgF2
Nanopore Filling
Si
Si
50 nm NPN
50 nm MgF2
Evaporation
RIE
5.4 x 5.4 mm chips
50 nm Au
Sputtering

## Slide 15: Superior Performance
Pixel
Credit: Flavius Pascut

## Slide 16: Write-Erase
Electroplate benzenthiol onto gold sensor
Read SERS
Reverse voltage on sensor, remove benzenthiol
Credit: Flavius Pascut
+/-

## Slide 17: Porous
100-200 cones in a 1000 nm spot

## Slide 18: Flow-through
SERS detectors are usually limited by Diffusive Transport!
Our transport is much better – small molecules can be ballistic
  Optimal dwell times?

## Slide 19: Flow-Through
Lsens
How do analytes reach the sensor?
Diffusion + Convection
L1
2
Eftekhari et al. “Nanoholes As Nanochannels: Flow-through Plasmonic Sensing”, Anal. Chem. 2009, 81, 4308–4311
1
L2
Move to sensor from bulk
Bind to sensor

## Slide 20: Flow-Through
Peclet Number =
  If Pe << 1, Convection Dominates
    Analyte moves quickly through sensor
  If Pe >> 1, Diffusion Dominates
    Analyte is depleted
Notes: Hard to compare different types of systems, use dimensionless numbers

## Slide 21: Flow-Through
Diffusion to wall
  D = 5e-6 cm2/sec
  Nanopore Diameter = L2 = 3e-6 cm
  = 1.8 μs
Diffusion through sensor
  Lsensor = 10e-6 cm
  = 20 μs
Lsens
0.1
Small scale flows can bring more analyte to the sensor without blowing past it!
L2

## Slide 22: Flow-Through
Diffusion Alone
Diffusion + Convection
6.4e-3 reactions/min
3.8e-2 reactions/min
Eftekhari et al. “Nanoholes As Nanochannels: Flow-through Plasmonic Sensing”, Anal. Chem. 2009, 81, 4308–4311
5 μL/min = 6x improvement
vs
Notes: SPR sensor, Tangential flows rate constant, 200 nm thick holely sensor

## Slide 23: Future Work
Model Structure
  How does the structure create the enhanced SERS properties?
  What molecules can be detected ideally?
Detect many different types of molecules
  Every molecule has a different crossection

## Slide 24: Summary
New Raman-silent nanomembrane materials are enabling some exciting biosensing!

## Slide 25: Acknowledgements
University of Rochester
Prof. James McGrath
Dean Johnson, PhD
Joshua Winans, PhD
Henry Chung, PhD
Tejas Khire
Karl Smith
Sarah Wayson
Meghan Kazanski
Tucker Burgin
J.P. DesOrmeaux
Josh Miller
Jamie Roussie, PhD
RIT
Prof. Tom Gaborski
Bob Carter, PhD
University of Nottingham
Prof. Kevin Webb
Flavius Pascut, PhD
Emilia Moradi, PhD
University of Ottawa
Prof. Vincent Tabard-Cossa
Kyle Briggs
URnano

## Slide 26: Questions?